# Product:			SPARKWELD NiFe

Classification:		AWS/ASME SFA-5.1	E NiFe CI

DIN 8573			E NiFe-1 BG-22

Application/Properties: Electrode with Nickel Iron core wire used for cold welding of

Iron. The weld metal is non machinable.

Suitable for: Grey Cast Iron.

White & Black Heart Malleable Cast Iron

Ductile Iron

High Strength Cast Iron

| Sizes and Currents AC or DC: | ## Diameter | Length | Current (A) |
| --- | --- | --- | --- |
|  | 2.6mm 3.2mm 4.0mm | 350mm 350mm 350mm | 60 - 80 80 - 120 110 - 150 |

| Weld metal analysis: | C | Fe | Ni |
| --- | --- | --- | --- |
|  | 0.50 | Balance | 55.0 |

| Mechanical properties of all weld metal: | Yield Strength | >300 N/mm2 |
| --- | --- | --- |
|  | Tensile Strength | 420 - 460 N/mm2 |
|  | Elongation | >10% |
|  | Hardness | HB 170 |

|  | 2.6, 3.2 & 4.0mm | 1x10kg. packet/carton |
| --- | --- | --- |
|  |  | 1 MT/pallet |