# Product:			SPARKWELD Ni

Classification:		AWS/ASME SFA-5.1	E Ni CI

DIN 8573			E Ni BG-22

Application/Properties: Electrode with Nickel core wire used for cold welding of Cast

Iron. The weld metal is machinable.

Suitable for: Grey Cast Iron.

White & Black Heart Malleable Cast Iron

Ductile Iron

| Sizes and Currents AC or DC: | ## Diameter | Length | Current (A) |
| --- | --- | --- | --- |
|  | 2.6mm 3.2mm 4.0mm | 350mm 350mm 350mm | 60 - 80 80 - 120 110 - 150 |

| Weld metal analysis: | C | Fe | Ni |
| --- | --- | --- | --- |
|  | 0.50 | 2.00 | Balance |

| Mechanical properties of all weld metal: | Yield Strength | >200 N/mm2 |
| --- | --- | --- |
|  | Tensile Strength | 380 - 420 N/mm2 |
|  | Elongation | >5% |
|  | Hardness | HB 140 |

|  | 2.6, 3.2 & 4.0mm | 1x10kg. packet/carton |
| --- | --- | --- |
|  |  | 1 MT/pallet |