

# Product: SPARKWELD Ni

**Classification:** AWS/ASME SFA-5.1 E Ni CI

 DIN 8573 E Ni BG-22

**Application/Properties:** Electrode with Nickel core wire used for cold welding of Cast

 Iron. The weld metal is machinable.

**Suitable for:** Grey Cast Iron.

 White & Black Heart Malleable Cast Iron

 Ductile Iron

|  |  |  |  |
| --- | --- | --- | --- |
| **Sizes and Currents****AC or DC:** | Diameter | Length | Current (A) |
| 2.6mm3.2mm4.0mm | 350mm350mm350mm | 60 - 8080 - 120110 - 150 |

|  |  |  |  |
| --- | --- | --- | --- |
| **Weld metal analysis:** | C | Fe | Ni |
| 0.50 | 2.00 | Balance |

|  |  |  |
| --- | --- | --- |
| **Mechanical properties****of all weld metal:** | Yield Strength | >200 N/mm2 |
| Tensile Strength | 380 - 420 N/mm2 |
| Elongation | >5% |
| Hardness | HB 140 |

|  |  |  |
| --- | --- | --- |
|  | 2.6, 3.2 & 4.0mm | 1x10kg. packet/carton |
|  | 1 MT/pallet |