# Product:			SPARK 7018-1

Classification:		AWS/ASME SFA-5.1 	E 7018-1

DIN 8529			E SY 42 76 M N B

EN499                   	  	E 42 6 B 42 H5

Application/Properties: Electrode for producing crack-free and tough welded joints with good toughness properties even on steels having carbon content up to 0.6%. Good operating characteristics also in positional welding. Weld metal exhibits good toughness properties down to -60 0C. Weld metal has very low hydrogen content and is resistant to ageing. Good gap bridging properties.

Suitable for:

Unalloyed structural steel: St33 to St52-3, St50-2 to St60-2.

Boiler Plates: HI, HII, 17Mn4

Pipe Steels: to St52.4, St35.8 to 17Mn4, StE210.7 to StE360.7 including corresponding TM-grades.

Fine Grain Structural Steels: StE255 to StE355, WStE255 to WStE355.

Shipbuilding Steels: A, B, D, E.

Cast Steel: GS-38 to GS-52.

Rebaking required at 250 – 350oC for two hours.

| Sizes and Currents AC or DC+: | ## Diameter | Length | Current (A) |
| --- | --- | --- | --- |
|  | 2.5mm 3.2mm 4.0mm 5.0mm | 350mm 450mm 450mm 450mm | 70 - 100 90 - 140 140 - 190 190 - 250 |

| Weld metal analysis: Typical Values | C | Si | Mn |
| --- | --- | --- | --- |
|  | 0.06 | 0.30 | 1.45 |

| Mechanical properties of all weld metal: Typical Values | Yield Strength | >420 N/mm2 |
| --- | --- | --- |
|  | Tensile Strength | 500 - 640 N/mm2 |
|  | Elongation L.=5D. | >22% |
|  | Impact Strength | 200 J at +20oC 60 J at –60oC |

| Packaging: | 2.6mm | 8x2.5kg.packet/carton |
| --- | --- | --- |
|  | 3.2, 4.0 & 5.0mm | 4x5kg. packet/carton |
|  |  | 1 MT/pallet |