# Product:			SPARK – E 8018-B2

Classification:		AWS/ASME SFA-5.5	E 8018-B2

EN ISO 3580-A		E CrMo1 B 42 H5

Application/Properties: Electrode for welding creep resistant steels of similar composition. Weld metal is of high purity and low hydrogen content. Creep resistant < 5700 c Welds are of X Ray quality.

Suitable for:

13 CrMo4-5, 13 CrMoSi5-5, G17CrMo5-5

| Sizes and Currents AC or DC+ | ## Diameter | Length | Current (A) |
| --- | --- | --- | --- |
|  | 2.6mm 3.2mm 4.0mm 5.0mm | 350mm 450mm 450mm 450mm | 70 – 100 90 – 140 140 – 190 190 - 250 |

| Weld metal analysis: | C | Si | Mn | Cr | Mo | P | S |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0.06 | 0.30 | 0.75 | 1.20 | 0.55 | 0.011 | 0.011 |

|  | 6900 c/2h | 9200 c/0.5h |
| --- | --- | --- |
| Mechanical properties of all weld metal: | Yield Strength | > 490 N/mm2 | > 300 N/mm2 |
|  | Tensile Strength | 560 - 690 N/mm2 | 450 - 550 N/mm2 |
|  | Elongation L.=5D. | > 23% | > 26% |
|  | Impact Strength | >120 J at +200C >80 J at -300C | >130 J at +200C >80 J at –300C |

| Packaging: | 2.6mm | 8x2.5kg.packet/carton |
| --- | --- | --- |
|  | 3.2 mm | 4x5.0 kg. packet/carton |
|  | 4.0 mm | 4x5.0 kg. packet/carton |
|  | 5.0 mm | 4x5.0 kg. packet/carton |
|  |  | ## 1 MT/pallet |