Class III SBR Waterproofing Membrane

KEMSEAL FCM

# DESCRIPTION

Kemseal FCM is a liquid applied fast curing SBR waterproofing membrane containing a fibrous filament reinforcing. * For non-exposed areas. When fully cured, Kemseal FCM forms a Class III flexible waterproof lining to showers and wet areas as described in AS 4858- 2004- ‘Waterproofing Wet Areas Within Residential buildings’ and AS 4654.02 2012, Exterior above ground. Kemseal FCM may be applied to most building materials including reinforced concrete, cement render, wet area plasterboard, compressed fibre-cement sheeting, plywood wet area flooring.

# PRINCIPLE CHARACTERISTICS

- Single component.

- Simple application.

- Flexible.

- Seamless- no joints or cracks.

- Fast cure.

- User Friendly- water-based.

# USE AREAS

- Shower Recesses

- Wet Areas

- Flashings

- Balconies and Decks

- Roof membrane – non-exposed

- Walls

# GENERAL.	 COVERAGE: 1.5 Hrs/sq.m(Floor)

# 0.8 Hrs/sq.m (walls)

SHELF LIFE:  2 Years

TOUCH DRY: 1-3 hrs +/-, @23⁰C

depending on temperature.

COLOUR: Grey or Blue RECOAT: 1-4 hours depending on atmospheric conditions

CLEAN UP: with water before dry.

SOLVENT RESISTANCE: Not Resistant

ELONGATION: 320%

WEATHER RESISTANCE: UV stable - may be top coated with Kemseal AC or other compatible water-based coating.

TILING: Kemforte FCM may be tiled over when fully cured with a compatible one or two-part cement-based adhesive. Externally, provide sufficient measures for full allowance of expansion and contraction in overlaying tiles and topping – particularly important with sheet flooring externally, or damage to the membrane may occur.

INSTALLATION

SURFACE PREPARATION: Ensure surface is firmly placed/fixed to manufacturers directions. Surface must be free of dirt, dust, loose particles, oil, contaminates, curing compounds and flaking concrete etc. Acid etch if necessary. Concrete must be a minimum strength of 20 mpa and have cured a minimum of 28 days. Surface must be dry.

PRIMER:  Prime external areas with Kemseal WBE. Absorbent internal surfaces should be primed with Kemseal ARW or with Kemseal WBE applied at 6 m2/Litre. Prime damp areas and areas subject to rising damp with Kemseal WBE. Plastic/Plumbing fittings shall be etched and primed with Kemseal WBE. Allow to fully cure prior to membrane application.

DETAILING: Install leak control flanges around all pipe penetrations. Fill all screw holes, cracks and voids with neutral cure silicone. To all corners such as wall/floor, floor/hob, hob/wall junctions, apply 12mm min cove of silicone sealant as a bond breaker. Apply sealant to internal wall/wall joints to 1.8m above the shower tray, around tap flanges and other discontinuities. Where angles are installed such as across bathroom doorways or under shower screens (hobless shower) angle is to be firmly adhered into a bead of sealant. Around pipe penetrations and floor waste outlets, apply membrane to 1.5mm thick reinforced with polyester fabric 100mm wide across join.

REINFORCEMENT / BONDBREAKERS: A reinforcing fabric and/or bondbreaker tape, should be used as necessary over the following areas: Expansion joints, cracks, footing/floor to wall junctions, shower tray and hob, joints in sheet flooring, vertical corners above shower tray, around floor/wall penetrations, down into floor waste pipes and any other area where movement will occur. Apply a bond breaking tape (eg 50mm PVC duct tape) over joints in sheet flooring, or 1.5 mm x 20mm wide silicone sealant. Reinforcement may also be required over voids in off form concrete.

Reinforcement shall be laid into the wet base coat and immediately over coated and worked in carefully to fully saturate fabric. Refer to Kemforte for full specification on expansion joints.

APPLICATION: To the prepared surface, apply Kemseal P14-Fibre by brush or roller in one or more coats to achieve a minimum dry film thickness of 1mm horizontally internal,  0.5mm shower walls and 1.2mm externally. This will require min.1.0-1.8L/m2. Turn membrane up at walls and penetrations and down into drainage outlets.

When dry, check for pinholes or misses and rectify if necessary. Re-coat when dry. If membrane becomes dirty or wet between coats, thoroughly clean or re-prime clean to ensure inter-coat adhesion. Allow to fully cure before covering- generally 2-4 days.

PRECAUTIONS: Do not use Kemseal P14-Fibre membrane in any situation beyond its physical limitations. Do not apply above 42°C or below 8°C ambient temperature. Wash equipment with water before dry. Do not fix tiles until fully dry. Protect membrane against damage before and during backfilling, tiling or covering. Where used externally, Kemseal 14-Fibre may be top coating with Kemseal AC or covered with tiles, sand-cement topping or soil etc. When tiled over externally, provide slip sheet of polyethylene plastic sheet over membrane prior to sand-cement topping, in a manner to allow for expansion and contraction of overlaying topping.

Disclaimer:The user is responsible to follow current data sheets. The information shown here is as up to date and correct in detail as possible and is intended to give a fair description of the product and its capabilities based on actual service history. In practice, the substrate and environmental conditions vary widely, making it essential for the user to determine the products suitability for a particular application and that the product is not used beyond its physical limitations. As the use of this material is beyond the manufacturers control, no guarantee expressed or implied is made as to such. Liability is limited to replacement of material proved faulty. Site Inspections, suggestions made or application instructions by Kemforte Systems, given verbally or in writing are always to be reviewed by; installers, contractors, consultants and building owners responsible for design and/or installation to ensure they are appropriate to the specific application or area of use, prior to application. Kemforte Systems terms and conditions of sale apply.

Email: sales@kemforte.com